SEMINARIUM Z MAGNETYZMU I NADPRZEWODNICTWA

Uprzejmie zawiadamiamy, że w środę

21 kwietnia 2021 r., o godz.10:00

odbędzie się seminarium on-line (link podany jest na stronie IF PAN),

na którym

prof. dr. Alexander Shengelaya

(Department of Physics, Tbilisi State University, Tbilisi, Georgia;

Andronikashvili Institute of Physics, Tbilisi State University, Tbilisi, Georgia)

wygłosi referat na temat:

## “Unusual normal and superconducting properties of tungsten oxide WO2.9”

In this talk I will present results of our studies of oxygen reduced tungsten oxides WO3-x. In the samples with one particular composition WO2.9 (W20O58) the signatures of superconductivity with the transition temperature Tc = 80 K were registered by means of magnetization measurements. After lithium intercalation the Tc further raised to 94 K [1]. The small superconducting volume fraction and the absence of clear transition in resistivity measurements indicate that the superconductivity is localized in small regions which do not percolate.  Performed resistivity and magnetoresistance measurements show that WO2.9 has also unconventional normal state properties, which can be understood by taking into account bi-polaronic nature of charge carriers in this compound [2].

[1] A. Shengelaya, K. Conder, K. A. Müller, J. Supercond. Nov. Magn. 33, 301  (2020).

[2] A. Shengelaya, F. La Mattina, K. Conder, Condens. Matter 5, 63 (2020).

Serdecznie zapraszamy

Roman Puźniak

Andrzej Szewczyk

Henryk Szymczak