SEMINARIUM Z MAGNETYZMU I NADPRZEWODNICTWA

Uprzejmie zawiadamiamy, że w środę

08 czerwca 2022 r., o godz.10:00

odbędzie się seminarium on-line (link podany jest na stronie IF PAN),

na którym

prof. dr hab. Andrzej Szewczyk

(Instytut Fizyki PAN, Warszawa)

wygłosi referat na temat:

“Magnetyczne przejście fazowe w TbAl3(BO3)4

poniżej 700 mK – jego kwantowe i klasyczne aspekty”

Co-authors: T. Zajarniuk, P. Wiśniewski, M. U. Gutowska, R. Puźniak , H. Szymczak, I. Gudim, V. A. Bedarev, M. I. Pashchenko, P. Tomczak , and W. Szuszkiewicz

Speciﬁc heat, CB, of a TbAl3(BO3)4 single crystal was studied for temperatures 50 mK < T < 300 K, with emphasis on the T < 1 K range, where a phase transition was found at 0.68 K. Nuclear, non-phonon, and lattice contributions to CB were separated. Based on the CB and magnetization, M, studies, we found that: (i) the phase transition shifts to lower temperatures with increase in magnetic ﬁeld B||, parallel to the easy magnetization axis, (ii) the critical, i.e., related to the phase transition, contribution to the speciﬁc heat, Ccr, shows an unusual dependence on T, , where y0 is a positive exponent, and (iii) the Grüneisen ratio, Γ, deﬁned as (S denotes entropy):

diverges for B|| approaching 0.6 T. The behaviors of both Ccr and Γ as a function of T (especially scaling of the latter for B|| ≥ 0.30 T) and of B|| are characteristic of the systems, in which the classical phase transition line is inﬂuenced by quantum ﬂuctuations, QF, and ends at a quantum critical point. By using the determined y0 and Γ values, we assessed the dynamical critical exponent z to be 0.82 ≤ z ≤ 0.96. Based on all the results, we suppose that QF dominate the behavior of the system and destroy the long range order, i.e., we suppose the transition found to have a quantum character.

The interpretation that we deal with the transition to the ferromagnetic order of Tb3+ magnetic moments is the most natural, intuitive, and supported by the M studies. However, such a transition should be smeared and shifted to higher T by B||, while we observe the opposite effect. Thus, other mechanisms can not be ruled out a priori.

The lecture will be given in Polish and the slides will be in English.

Serdecznie zapraszamy

Roman Puźniak

Andrzej Szewczyk

Henryk Szymczak