SEMINARIUM Z MAGNETYZMU I NADPRZEWODNICTWA

Uprzejmie zawiadamiamy, że w środę

05 października 2022 r., o godz.10:00

odbędzie się seminarium on-line (link podany jest na stronie IF PAN),

na którym

dr hab. inż. Witold Skowroński, prof. AGH

(AGH University of Science and Technology, Institute of Electronics, Kraków, Poland

CIC nanoGUNE, San Sebastian, Basque Country, Spain)

wygłosi referat na temat:

“Zjawiska związane z oddziaływaniem

spinowo-orbitalnym

w strukturach cienkowarstwowych”

Efficient generation, control and detection of the spin currents is essential in a new class of spintronic devices that can serve as energy efficient replacement of conventional electronic memories and computing platforms [1]. Strong spin-orbit coupling existing in a range of materials such as heavy metals, 2D van der Waals structures or topological insulators enables generation and detection of the spin-polarized current with different symmetries. Such spin current can be used to control the magnetization state of thin film heterostructures leading to the magnetization switching or oscillations by spin-orbit torques (SOT). In this talk, I will present current trends and challenges in SOT hybrid heterostructures. I will address SOT magnetization switching and SOT-induced magnetization precession. Various engineering methods of the thin films structure will be presented to obtain external magnetic field-free magnetization switching, for example by using antiferromagnets, combination of spin transfer torque and SOT and by utilizing interlayer coupling between ferromagnets [2-3]. In addition, I will focus on the unconventional torque symmetries observed in van der Waals heterostructures [4] and low symmetry crystals [5]. Finally, I will discuss the combination of SOT and the multiferroic properties of LSMO/BTO-based [6] magnetic tunnel junction and the possible pathways towards the electric-field control of spin currents.

The author acknowledges collaborators from AGH University: S. Łazarski, K. Grochot, J. Mojsiejuk,

P. Rzeszut, S. Ziętek, J. Kanak, T. Stobiecki, J. Pawlak and M. Przybylski, from IPM PAS Poznań, Poland: P. Kuświk and F. Stobiecki, and from CIC nanoGUNE, San Sebastian, Spain: M. Sharma, M. Gobbi,

F. Casanova and L. Hueso. The project is supportedy: by the National Science Centre, Poland Grant No. UMO-2021/40/Q/ST5/00209, by NAWA Bekker program No. PPN/BEK/2020/1/00118/ZAS/00001, and by program “Excellence initiative – research university” for the AGH University of Science and Technology.

[1] – B. Dieny et al. Nature Electronics 3, 446 (2020)

[2] – S. Łazarski et al. Phys. Rev. Applied 12, 014006 (2019)

[3] - S. Łazarski et al. Phys. Rev. B 103, 134421 (2021)

[4] – D. MacNeill et al. Nature Physics 13, 300 (2016)

[5] – L. Liu et al. Nature Materials 16, 277 (2021)

[6] – J. Pawlak et al. Adv. Electron. Materials 8, 2100574 (2022)

The lecture will be given in Polish and the slides will be in English.

Serdecznie zapraszamy

Roman Puźniak

Andrzej Szewczyk

Henryk Szymczak